## Slide 1
Si substrate
Purchase 200 µm thick DSP Si wafer
with 0.5 µm of low-stress Si3N4 (“SiN”). Deposit photoresist (PR) and expose through “Nb Plug” mask. This changes the chemical properties of the exposed photoresist.
Cross Section
Top View
Remove mask, develop photoresist (i.e. remove exposed part) and deposit Nb over entire wafer.
Remove (“lift off”) PR and the Nb on top of it. This transfers the pattern from the “Nb Plug” mask onto the Nb.
Si substrate
Si3N4
Photoresist
Si substrate
Photomask with “Nb Plug” pattern
Nb
Plug
Plug
Si3N4
Si3N4

## Slide 2
Deposit Al-Al2O3-Al trilayer. (The first section of Al base layer is thermally evaporated so that Al sticks to SiN.)
Cross Section
Top View
Spin on photoresist and expose it to UV through “Base electrode” mask.
The mask also contains patterns for base electrode wiring (interrupted by the Nb block) and bond pads.
Si substrate
Al wire bond pads
STJ
Photoresist
Si substrate
Al
Al
Al2O3
Plug
Al
Al
Al2O3
Plug
Mask with “Base electrode” pattern
Si substrate
Al
Al
Al2O3
Plug
Remove mask, develop PR and etch through top Al electrode and Al2O3 tunnel barrier, but only partially into the base Al electrode (timed etch). Remove remaining (unexposed) PR.
STJ

## Slide 3
Remove photoresist (PR), spin on new layer of PR and expose through “top electrode” mask, whose area is a bit smaller than the base electrode. The mask includes a section above the Nb plug to make Al wiring discontinuous.
Si substrate
Remove mask, develop photoresist (i.e. remove exposed part) and do a timed etch through top electrode and tunnel barrier. This also removes base electrode from previously etched areas. Passivate STJ edges by anodization before removing PR.
STJ
Mask with “top electrode” pattern
Si substrate
Al
Al
Non-anodized wire bond pads
Anodized
STJ
Base layer wiring
STJ
Si substrate
Deposit “Nb wiring” by lift-off, i.e. spin on PR, pattern and remove exposed PR in area where we want the Nb wiring to be. Deposit Nb on top of PR, remove PR to leave Nb behind in area without PR.
Nb
wiring
Nb wiring
to top electrode.
Al
Al2O3
Plug
Al
Plug
Plug
Is this correct? Do all bond pads have a buried junction so that they don’t get anodized?
Anodized oxide

## Slide 4
Si substrate
Nb
wiring
Plug
STJ
STJ
(Absorber optional)
Au thermalizer
SiN on Si
SiN membrane
Si substrate
Nb
wiring
STJ
(On EXAFS pixels only): Pattern lift-off mask for absorbers, deposit Ti seed layer, fully oxidize it and deposit Pb by lift-off.
Pb absorber
(EXAFS only)
Au bond
pads
Frame and connections for anodization
Alignment
marks
Pattern back side of wafer, reactive-ion-etch through Si until Si3N4 to form membrane.
Si3N4
Spin on and pattern PR using “bond pad” mask. This also provides the pattern for Au thermalizer. Deposit thin Ti sticking layer and thick Au bonding / thermalization layer and pattern by life-off.
STJ
Nb
wiring
STJ
Si3N4 membrane
Si substrate
STJ
Plug
Bond pad
Pb absorber
(EXAFS only)
Completed Al-STJ
SiN membrane
Al-STJ
Au thermalizer
Nb plug
SiN
on Si
Al
wiring
Nb
wiring
Base electrode
wider than top el.